비상용 고분자 계면에서 상용화제의 역할에 관한 이론적 연구

임광모, 차국헌

서울대학교 화학공학과

A Theoretical Study of the Role of Compatibilizers at Immiscible Polymer Interfaces

Kwangmo Lim and Kookheon Char

Department of Chemical Engineering

Seoul National University

Introduction

Polymer blending is used as one of convenient methods to produce a material with desirable properties.  Most polymer pairs are however immiscible and form phase-separated structures when mixed together.  The phase-separated blends are in general useless because the interface between the immiscible polymers is quite fragile.   In order to obtain  polymer blends with desirable properties, it is quite important to control the structures of interface.  One method of achieving this goal is the addition of the proper compatibilizer at the interface.

One of commonly need compatibilizers is the diblock copolymer each block of which  has an affinity with relevant polymer phase [1].  Such diblock copolymers tend to segregate at the interface because of energetic interaction and this segregation of the diblock copolymer lowers the interfacial tension, enhances the adhesion between both immiscible polymer phases and makes the disperse phase finely dispersed in a continuous phase.

Recently, reactive compatibilizers with proper functional groups are preferred since one does not need to make copolymers separately and it is also possible to play a role of a compatibilizer during processing of polymer blends [2].

In present study, we would like to study the effect of a diblock copolymer on the interfacial properties such as interfacial tension as a functions of molecular weight of copolymer, Flory-Huggins interaction parameter () and the amount of copolymer added at the interface between immiscible homopolymers.  Since it is possible that the phenomena of the reactive compatibilzation are considered as those of the adsorption of polymer having tan end functional group, we would like to learn about the behavior of the reactive polymers at interface with an analygy to the polymer adsorption.

Theory

The self-consistent mean field (SCMF) theory developed by Shull and coworkers has been reported in many papers [3,4].  We modified the theory by Shull et al. to take into account the behavior of copolymer at the interface properly.  We will briefly describe the theory here in case of A-B diblock copolymer present at the interface between A and B homopolymer.  The adsorption of polymer can also be studied through the modification of this theory.

The distribution function of copolymer qk(i,j) can first be obtained from the modified diffusion equation initially suggested by Edwards [5].  It is possible to convert the modified diffusion equation into a descrete form when a cubic lattice is employed. The subscript k corresponds to the type of polymer, i is related to the position and j to time step.

qk(i,j)=16qk(i−1,j−1)+46qk(i,j−1)+16qk(i+1,j+1)exp(−wk(i)kBT)

The function wk(i)is the position-dependent mean field which is in turn related to the local composition.  The expression for the mean field can be obtained from the Hong and Noolandi theory.

wk(i)=mk(i)Nk−kBTNklnfk(i)−Dw(i)

mk(i) means the chemical potential which is obtained from the Flory-Huggins equation [6].

The volume fraction is calculated from following equation.

fk(i)=AkNkjqk(i,j)qk(i,Nk−j)

Ak is a proper normalized constant related to the volume fraction of bulk phase.

As shown above, the distribution function is related to the mean field and mean field is also obtained from volume fraction which is calculated  from the distribution function. Consequently, we are to obtain the result by self-consistent calculation.

Finally, the interfacial tension is obtained from the equation derived by Hong and Noolandi [7].

DgakBT=ifc(i)Nclnfc(i)fcBulk−fc(i)−fcBulkNc−12cfpBulk(fc(i)−fcBulk)

Result and Discussion

The theory developed by Shull can be applied to various systems by proper modification .  Based on the Shull’s theory, we studied several systems including A/B diblock copolymer present at immiscible homopolymer interface.  Only brief results are presented here..

Fig. 1 is the profile of each copolymer block calculated from the theory explained above and the interfacial tension and excess amounts of copolymer at the interface are also obtained from the profile.  As shown Fig. 1, the amount of copolymer at the interface increases as chemical potential of copolymer is increased.

Fig. 2 (a) shows the relationship between the interfacial tension and the excess amount of copolymer as a function of various degrees of polymerization of the copolymer. The copolymer having a lower degree of polymerization is more efficient than that having a higher molecular weight since the number of chains is larger for a shorter chain for a given amount of copolymer at the interface.  To understand what is more efficient for the same number of chains at interface, we divide the excess amount of copolymer by the degree of polymerization. When the number of copolymer at the interface is fixed to be same, the longer copolymer is somewhat more efficient than the shorter one as shown in Fig. 2 (b).

The effect of interaction parameter on interfacial properties and the calculation results  for the adsorption of polymer containing a functional group at the end which has an affinity to surface will also be presented.

Reference

1. Fayt, R.; Jerome, R.; Teyssie, PH. J. Polym. Sci. Polym. Phys. Ed. 1989, 27, 775.

2. Guegan, P.; Macosko, C. W.; Ishizone, T., Hirao, A.; Nakahama, S. Macromolecules

1994, 27, 2646.

3. Shull, K. R.; Kramer, E. J. Macromolecules 1990, 23, 4769.

4. Shull, K. R. J. Chem. Phys. 1991, 94, 5723.

5. Edwards, S. F. Proc. Phys. Soc. London 1965, 85, 613.

6. Hong, K. M.; Noolandi, J. Macromolecules 1980, 14, 727.

7. Noolandi, J.; Hong, K. M. Macromolcules 1984, 17, 1531.

Fig. 1. The effect of chemical potential on the interfacial profiles of copolymer.

2 kBT,       4 kBT,      6 kBT

(a)                                   (b)

Fig. 2. The effect of the molecular weight on the interfacial tension.

NCA=200,       NCA=500,      NCA=1000