탄소/탄소 복합재료에서의 Molybdenum disilicide 분말의 영향

박수진, 박원배, 이재락

한국화학연구소 화학소재연구단

Influence of Molybdenum disilicide Powders on Carbon-Carbon Composites

Soo-Jin PARK, Won-Bae PARK, Jae-Rock LEE

Advanced Materials Division, Korea Research Institute of Chemical Technology

# Introduction

Carbon fiber reinforced carbon matrix composites (C/C composites) has been widely used in many fields due to their excellent mechanical properties, chemical stability and thermal stability. So they are developed due to the demands of the aircraft and aerospace industries. Their use as rocket propulsion components, reentry tips, exhaust cones and friction pads leads to the evaluation of their ablation performance[1].

Phenolic resin is a versatile group of materials that meet extended requirements both in properties and processing. They are commonly used as starting materials, in the resin-based process, C/C composites preparation by a procedure employing pyrolysis and carbonization of resin matrix and subsequent densification. Since they are easy to handle and give considerable carbon char yield[2].

In their real applications, the study on oxidation reaction inhibition for the prediction of C/C composite working life in oxidizing environments is one of the primary concerns for the prediction of composite behaviors along with the study of thermal and mechanical properties of C/C composites. On the other hand, silicides like MoSi2 may be more suitable for this application, as these materials have high melting point (>2300K) and excellent oxidation resistance. In addition these materials becomes ductile above its brittle-to-ductile transition (BDT) temperature of 900℃[3], leading to the high mechanical performance at high application temperatures.

The objective of the present work is to provide understanding of the effects of the ceramic powders on the oxidation reaction inhibition. Also, thermo-mechanical properties carried out from differential scanning calorimeter (DSC) and thermo-gravimetric analysis (TGA), and the results of scanning electron microscopy (SEM) and density-porosity changes of the C/C composites with and without ceramic powders will be discussed.

Experimental

PAN-based high strength carbon fibers (Toray, T-300, 6K) were used in the form of plain weave from the fibers of which were treated through commercial standard surface oxidation. The resole type of phenolic resin was used as the matrix precursors of C/C composites to be studied. The MoSi2 powders (<1㎛, supplied from Aldrich Co.) were used as the oxidation inhibitor of C/C composites and prepared by taking 0, 5 and 10phr. of MoSi2 on the basis of C/C composites.

The green composites from the sixty plies of resin impregnated carbon fabrics were prepared in a hot-press at 10.5MPa. and 470K for 60min. Five subsequent densification cycles carried out by the liquid phase impregnation and carbonization of up to 1270K, were performed in order to increase the bulk density of C/C composites. The heating rate to the carbonization temperature was fixed to 2K/min. The carbonization retention time of the specimens at 1270K was 128min.

The oxidation inhibition properties of C/C composites were characterized from the weight loss changes of specimens by using TGA of up to 1170K in oxidizing environments.

The mechanical behaviors of C/C composites were characterized by the three-point bending test for flexural strength and modulus properties (s/d=16, c.h.s=1.0mm/min). The interlaminar shear strength (ILSS) of the composites between fiber and matrix and/or ceramic powder were characterized by the shot-beam test for the degree of adhesion at the interfaces (s/d=4, c.h.s=1.0mm/min).

Results and Discussion

Fig. 1 and Fig. 2 exhibits the results of bulk density and flexural modulus measured as a function of the number of densification cycles for all composites studied. As expected, the increasing of bulk density is closely related to the growing of flexural modulus of the composites. Also it is seen that at the composites made with MoSi2, the bulk densities are higher than those of the composites unmade with MoSi2 as a function of densification cycles. And the increasing of the amount of MoSi2 in C/C composites shows the decreasing of apparent porosities of the composites. This is due to the presence of MoSi2 in open and closed pores of the composites, as shown in Fig. 3, studied by SEM.

While it is generally accepted that good mechanical properties and long durability of the composites largely depend on fiber-matrix and/or fiber-matrix-filler interfacial adhesion in the case of the fiber reinforced matrix composites, since the transferring load stress from the matrix to the fiber would require the strong adhesion at the interface of the constitutive elements rather than high cohesive density. The degree of adhesion at the interface between fiber and matrix may be measured by the short beam test for ILSS of the mechanical behaviors.

From the ILSS results as shown in Fig. 4, the presence and the increasing of the amount of MoSi2 lead to the increase of ILSS of C/C composites. From which, it can be concluded that the effects of the amount of MoSi2 on the composite properties are twofold: it increases the adherent surface areas between fibers-matrix-ceramic powders (or it decreases the porosities between fibers and matrix) and it allow the BDT behavior which is an intrinsic properties of MoSi2.

References

- Donnet, J.B. and Bansal, R.C., “Carbon Fibers”, 2ed., Marcel Dekker, New York (1990).

- Knop, A. and Pilato, L.A., “Phenolic Resins”, Springer-Verlag, Berlin (1986).

- Jandhyala, S., J. Am. Ceram. Soc., 76, 226 (1993).

Figure 1. Evolution of bulk density measured as a function of the densification.

Figure 2. Evolution of flexural modulus measured as a function of the densification.

Figure 3. Evolution of ILSS measured as a function of the densification.

(a) 0phr.                                                              (b) 5phr.

Figure 4. Scanning electron microscopy of C/C composites with MoSi2.