- 여러 흡착제상에서 MEK의 비등온 흡착거동

- 심왕근, 양우철, *양재호, 문 희

- 전남대학교 응용화학공학부

*전남대학교 화학공학과

- Non-Isothermal Adsorption Behavior of MEK on Various Adsorbents

- Wang Geun Shim, Woo Chul Yang, *Jai Ho Yang, Hee Moon

Faculty of Applied Chemical Engineering, Chonnam National University, Kwangju 500-757

*Department of Chemical Engineering, Chonnam Natioanl University, Kwangju 500-757

- Introduction

Adsorption of Volatile Organic Compounds (VOCs) from air has been studied for a long time since VOCs have been known as a major contributor to photochemical smog, which can cause haze, damage to plant and animal life, and eye irritation and respiratory problem for humans. VOCs are used as solvents in manufacturing conuntless products (ex, crystallized organic chemicals, printed materials, paints and coatings, and dry-cleaning fluids). One consequence of these manufacturing operations is that large amounts of organics are being emitted to the atmosphere each year. Therefore, VOCs are among the most common pollutants emitted by chemical process industries. Accordingly, VOC emission control is a major portion of environmental activities. Therefore the proper recovery of volatile solvent vapors from industries has multiple purposes such as reduction of production cost, energy saving, and environmental protection.

In Korea, about 1000 tons of various solvents in a year have been used in many industrial processes as polyethylene coating and cleaning agents. The emissions from some industries contain BTX, MEK, and other valuable solvents which should be recovered to reduce production cost and air contamination.

The primary objectives of the present work are the recovery of a solvent vapor by a adsorption process and the theoretical analysis of adsorption bed dynamics based on a mathematical model. The purpose of the present work is to obtain the pertinent adsorption and desorption data and to develop a mathematical model for the calculation of a non-isothermal adsorption process. An activated carbon, MS-13X (sphere, pellet), a silica gel, MS-4A, a polymeric resin (SP850) were used as adsorbents and a volatile organic compound, MEK, was chosen as a solvent.

- Theoretical Model

The mathematical model of a non-isothermal, dynamic-column adsorption process basically requires transient material and energy balances. In this regard, both the adsorption equilibrium and kinetic aspects of the process must be accounted for. The model adopted here utilizes the Langmuir isotherm equation and a linear driving force (LDF) rate model to simplify the diffusional mass transfer inside adsorbnet particles. The LDF model is a lumped-parameter model for particle adsorption.

A simple model for a non-isothermal adsorption in a fixed bed is as follows;

- Mass balance:

(1)

- -DL∂2C∂z2+v∂C∂z+∂C∂t+1−εερp∂q∂t=0

Heat balance, with axial thermal conduction:

(2)

−Kzε∂2T∂z2+vρgCg∂T∂z+ρgCg+1−εερgCs∂T∂t−(−ΔH)1−εε∂q∂t+2hεR(T−T0)=0The mass-transfer rate inside particles can be represented by

(3)

∂q∂t=Ks(q∗−qs)

The Langmuir equation is used for adsorption equilibrium

(4)

q∗qs=bC1+bC

The PDEs representing the packed bed dynamics were solved by a numerical method called “method of lines (MOL)”. Eqs. 1-4 were first reduced to a set of ordinary differential equations (ODEs) by the method of lines. The resulting set of ODEs were integrated in terms of time using the subroutine LSODE of the International Mathematical and Statistical Library (IMSL).

- Experimental

The system in the present study was used for various adsorbents (activated carbon, MS-13X (sphere, pellet), silica-gel, polymeric resin(SP850), MS-4A) and M.E.K. The apparatus was constructed with stainless steel tubes. The gas flow line of nitrogen was divided into three branches, one is for pure nitrogen gas and the others are connected to solvent saturators. A Hakke constant temperature circulator (F4391) was attached to the saturators in order to maintain their temperature. The concentrations of each solvent were evaluated from its saturated vapor pressure at a given temperature by assuming its vapor-liquid equilibrium state. All lines were sufficiently heated (more than water bath) to prevent the saturated solvent vapors from condensing in the steel tubes. The gas mixture of saturated solvent vapors and  pure nitrogen gas was delivered to the adsorption section. The gas flow through the column was controlled by mass flow controllers with a read-out power supply which was precalibrated against a soap bubble flow meter covering a wide range of flow rates under experimental pressures. The gas mixture was heated to the experimental temperature in the preheating section before being charged to the fixed-bed adsorber. Two K-type thermocouples were installed at inlet and outlet sections of the packed column, and the temperatures were monitored continuously on a display recorder. The composition of exit gas stream from the adsorption section was determined using a gas chromatography, GC-14B model (Shimadzu), equipped with a hydrogen flame ionization detector. Helium was used as a carrier gas.

- Results and Discussions

Experimental adsorption and desorption runs were performed for various adsorbents. The operating conditions for all runs are as follows; T = 35oC, Co = 3.0mol/m3 and W (loading weight) = 3g.

Fig. 1 shows the adsorption breakthrough curves for various adsorbents. Activated carbon is superior to other adsorbents in the adsorption capacity. Also, MS-13X (sphere) and silica-gel have nearly the same adsorption capacity less than that of activated carbon. Fig. 2 shows the desorption breakthrough curves for various adsorbents. The desorption was performed at the same flow rate used in the adsorption. The practical wash out of the column requires more than twice the time of adsorption. But, in the case of MS-13X (sphere), the wash-out time of the column is the same as that of adsorption. Fig. 3 shows the temperature curves for the various adsorbents. The range of temperature rise is about 1~6oC. The temperature rise on MS-13X (sphere) is about two times of that on activated carbon. Fig. 4 shows experimental and simulation breakthrough curves of MEK from the column charged with activated carbon. The non-isothermal model used here predicts experimental results reasonably as shown in Fig. 4. It is clearly shown from Fig. 4 that both thermal and concentration curves appear at the end of the column simultaneously.

- References

1.  Farooq, S.; Ruthven, D.M. Ind. Eng.Chem.Res., 29, 1084 (1990)

2.  Hwang, K. S., Choi, D.K., Gong, S.Y., Cho, S.Y. Chem.Engng Sci. 52, 1111 (1997)

3.  Ruthven , D. M., “ Principles of Adsorption and Adsorption Process ”, Wiely, New York  (1984)

FFigure 1. Adsorption breakthrough curves of M.E.K for various adsorbents. (Co= 3.0mol/m3

,      , Temp = 35oC )

Figure 2. Desorption curves of M.E.K for various adsorbents

Figure 3. Temperature curves.

Figure 4. Experimental and simulated breakthrough curves of M.E.K for activated carbon columns.