이중 블럭 고분자 (라멜라 구조) 박막의 형상에 대한 연구

김 연상, 서 갑양, 이 홍희

서울대학교 화학공학과

Morphology of Thin Films of Lamellar Diblock Copolymers

Y. S. Kim, K. Y. Suh and Hong H. Lee

Department of Chemical Engineering ,Seoul National University

1. Introduction

It is well known that the morphology of thin films of diblock copolymers is different from that of bulk copolymer. In thin films, surface and strain effects due to lattice mismatch come into play. Various morphologies that result when a thin film of lamellar diblock copolymer is confined between two hard parallel surfaces have been studied.[1,2,3] When the film surfaces are not confined, however, different morphologies result. For a thin films on a substrate with a free exposed upper surface, islands (or holes) form on the free surface due to stress.[4-8] The formation of islands (or holes) requires the interface to deform and stretch (increase area), as shown in Figure 1, and this deformation increases the surface energy. On the other hand, the formation leads to relaxation of strain such that the total energy decreases in the process of island formation. It is well known that the height of the island is equal to the equilibrium lamellar periodL0.[4,5,7,9,10] It is not known, however, what the period is for the underlying lamellar structure. While such a morphology has been observed for thin films, a flat free surface results when the film is relatively thick.[11]

In this note, a criterion is derived for the conditions for island formation or flat surface. In the process, the question regarding the period of underlying lamellar structure is resolved.

2.Theory

We define the lattice mismatch,f, as follows :

f=(L0−L)L0                              (1)

where L0 is the equilibrium period of the diblock copolymer and L is the period adjusted to film thickness. Then the strain energy in one dimension, Est, is given by

Est=12Gf2tA                          (2)

whereG is Young’s modulus, t is the film thickness and A is the surface area. The surf-ace energy due to island formation, Esf, is

Esf=gAA'                              (3)

whereA' is the area of deformed free surface and gA is the surface tension. From above equations, it follows that the total energy per unit area (EA) is

EA=EstA+EsfA=12Gf2t+gAA'A=12GL0−LL02t+gAA'A    (4)

If L is not consistent with L0, islands (or holes) form on the free surface due to stress. In the initial roughening stage, the free surface is deformed as shown in Figure 2 and then the islands (or holes) grow on the surface. The initial stage of island formation, as in Figure 2 b), is metastable. If the increase in surface energy is larger than the decrease in strain energy [Figure 2 b)], islands (or holes) cannot be formed. The increase in surface area in the initial stage of island formation is

A'−A=nL'−LApL022L0pL02=nL'−LA4L0                  (5)

where L' is the period adjusted to the initial film thickness (t=nL'). The total energy per unit area (EA) in the initial stage of island formation is

EA=12GL0−LL02nL'+gA4nL'−L1L0+1            (6)

The minimum of the energy with respect to the period L can be obtained by setting the first derivative equal to zero. Because of the term, L'−L, two cases arise, i.e., when L'−L>0 and when L'−L<0. For L'>L, the first derivative is

¶(EA)¶L=−nL0GL0−LL0L'+4gA                    (7)

and the period of the film corresponding to the minimum energy is

L=L0+4gAL0GL'ºLmin                              (8)

which follows from Eq. (7), when it is set to zero.

The island topography should result if the corresponding energy is less than the energy corresponding to the flat topography, (EA)flat, i.e.,

(EA)isle<(EA)flat                             (9)

where (EA)isle is the minimum energy of Eq. (6) corresponding to Lmin. The energy (EA)flat is simply (EA) given by Eq. (6) with L replaced by L' since the surface would remain flat when L=L'. But (EA)isle is the minimum of Eq. (6) in the interval, L0<L<L', and therefore Eq. (9) is automatically satisfied. Thus, the condition for the island formation is that a minimum with respect L exists in the interval, L0<L<L'. This condition is

Lmin<L'                                 (10)

With the aid of Eq. (8), the condition can be rewritten as follows :

4β<(L'−L0)L0βºgA(GL')                            (11)

When L'<L, the period L corresponding to the minimum energy is

L=L0−4gAL0GL'ºLmin                          (12)

By the same reasoning as in the case of L<L', the criterion for island formation can be written as follows :

4β<(L0−L')L0                            (13)

Finally, the criteria for the two cases can be combined into

4β<L'−L0L0                            (14)

In this light, take as an example the experimental data by Coulon et al.[6] for the use of the criterion. The diblock copolymer they used is polystyrene (PS)-polymethylmethacrylate (PMMA) with an equilibrium period of 39 nm. The initial film thickness was nearly 70 nm and the morphology that resulted after 47 hours of annealing was island structure. The initial period of the film L' was 46.7 nm. The parameter values are gPS=33ergcm2 and G=3300Nmm2 (PS). Therefore, β=2.14´10−4. Substitution of these values into Eq. (14) shows that the condition is satisfied, which means that the island structure should result as the experiment indicates.

For a given system, one single parameter, β, which is a dimensionless length, determines the morphology. Note in this regard that the critical film thickness at which the morphology goes through a change can also be determined from Eq. (14).

In general, the film thickness t is incompatible with the equilibrium period L0, i.e., t¹nL0, where n is either an integer for symmetric case or an integer plus one half for antisymmetric case, such that the period adjusts to L. Therefore, the number of repeating layers n is related to the film thickness as follows :

t=(n+α)L0                                (15)

On the other hand, t=nL'. Therefore, when 0<α<n(2n+1), the ratio L'−L0L0 becomes α/n. When n(2n+1)<α<1, however, the ratio becomes (1−α)(n+1). Thus, the criterion in terms of thickness or n is

4β<BBºalignlαnfor0<α<n(2n+1)                 (16)

The critical film thickness is that corresponding to the value of n that satisfies the condition of Eq. (16). This critical thickness or n is shown in Figure 3 for the example considered earlier for two values of α. When the film thickness is sufficiently large such that the value of B approaches zero, the condition is violated and the flat surface results.

3. Conclusion

In summary, a criterion has been derived for determining the morphology of unconfined lamellar diblock copolymers. The critical number of layers leading to the island structure can be determined. The period of the underlying film for the island structure has been derived.

4. References

- Walton, D. G., Kellogg, G. J., Mayes, A. M., Lambooy, P. and Russell, T. P. Macromolecules   1994, 27, 6225.

- Kellogg, G. J., Walton, D. G., Mayers, A. M., Lambooy, P., Russell, T. P., Gallagher, P. D. and Satija, S. K. Phys. Rev. Lett. 1996, 76, 2503.

- Turner, M. S. Phys. Rev. Lett. 1992, 69, 1788.

- Collin, B., Chatenay, D., Coulon, G., Ausserre, D. and Gallot, Y. Macromolecules 1992, 25, 1621.

- Maaloum, M., Ausserre, D., Chatenay, D., Coulon, G. and Gallot, Y. Phys. Rev. Lett. 1992, 56, 68.

- Coulon, G., Collin, B., Ausserre, D., Chatenay, D. and Russell, T. P. J. Phys. France 1990, 51, 2801.

- Koneripalli, N., Singh, N., Levicky, R., Bates, F. S., Gallagher, P. D. and Satija, S. K.  Macromolecules 1995, 28, 2897.

- Singh, N., Kudrle, A., Sikka, M. and Bates, F. S. J. Phys. Ⅱ France 1995, 5, 377.

- Mansky , P. and Russell, T. P. Macromolecules 1995, 28, 8092.

- Mayers, A. M., Russell, T. P., Bassereau, P., Baker, S. M. and Smith, G. S. Macromolecules 1994, 27, 749.

- Coutandin, J., Ehlich, D., Sillescu, H. and Wang, C. H. Macromolecules 1985, 18, 589.

Figure 1. Island formation in diblock 	  Figure 2. Island formation process from the

copolymer film at equilibrium.	  initial roughening stage to the equilibrium state :

a) initial roughening stage, b) initial stage of island

formation and c) island growing stage.

Figure 3. The morphology of diblock copolymer. The parameters are :β=2.14´10−4 and 0<α<n(2n+1). When 4β<B, islands form. When 4β>B, however, the free surface remains flat.