Specific Interaction 이 상거동에 미치는 영향

이용석, 배영찬

한양대학교 응용화학공학부 분자열역학 연구실

## Effect Specific Interaction on the Phase Behavior

Yong Seok Lee, Young Chan Bae

Division of Chemical Engineering and Molecular Thermodynamics Lab.

Hanyang University, Seoul 133-791, Korea

# Introduction

Phase behaviors of nematic liquid crystals (EBBA (P-ethoxy-benzylidene-p-n-butylaniline)) in linear polystyrene ( PS ) are investigated by thermo-optical analysis ( TOA ) technique. We employed a generalized lattice fluid model to describe the specific interaction between liquid crystal and polymer. new model by combining Ballauff’s model with the generalized lattice fluid model is proposed. The model used in this work includes two adjustable model parameters (ε,δε12). Results are compared with the proposed model.

# Theoretical Considerations

 Ballauff model

The combinatorial analysis along the lines given by Flory may be readily adapted for the system under consideration. As usually, the mixing partition function ZM is subdivided into a combinatorial, an orientational, and a configurational part.

ZM=ZCombZOrientZConfig                                    (1)

whereZconfig is a constant. Thus, this treatment excludes the possibility of any ordering effect of the nematic phase on the polymer coils residing therein. The quantity y specifies the disorientation of the rodlike paritcles. For a molecule with the long axis at an angle ψ with respect to the domain axis.

y=4πxrsinψ                                      (2)

ZM=n0−nx(xr−y)!n0−nxxr!nx!n0nx(y−1)Zorientn0−nxxr!n0−nxxr−ncxc!nc!n0nc(xc−1)         (3)

The orientational partition function Zorient may be expressed as :

Zorient=Πyωynxnxyexp(−xrεy/2kBT)nxy                            (4)

εψ=−(kBTV)νrs(1−32sin2ψ)                                  (5)

Isotropic energetics may be included in the form of a characteristic temperature for an isotropic interaction and it is shown as :

ΔHM=ncxcvrTisoT=ncxcvrχ                              (6)

 The proposed model

The number of arrangements of the N12 pairs on the lattice is 1+g12N12. In the absence of energetic preferences the probability Pθ that θ of these interactions are specific and 1−θ are nonspecific is given by the combinatorial expression

Pθ=N12!θN12!1−θN12!g121−θN121+g12N12                          (7)

Note that Pθ=1. The partition function Z12 associated with this 1-2 interaction is

Z12=PθexpN12βε+θδε12                         (8)

Approximating Z12 by the generic term in the sum defines f12 as

f12=ε+θδε12−kTθlnθ+1−θln1−θ/g12+ln1+g12           (9)

Minimizing F12 with respect to θ yields

θ=1+g12exp−βδε12−1                                 (10)

f12=ε+δε12−kTln1+g121+g12exp−βδε12                      (11)

f12=z2f12                                           (12)

f∗z21+2δε12ε1T+2ln1+g121+g12expδε12εT                    (11)

 Chemical Potential

Anisotropic phase

Δμr'RT=lnνr'xrVr+νr'(y−1)+νc'xr1−VrVcxc+xrVrV'−1+xr(Vr−1)a+ln1−1V'

−lnf1−xrνr'sV'θ1−12s−12sνr'1−V'Vr+12sνc'

+z21+2δε12ε1T+2ln1+g121+g12expδε12εT11−bνr'2νcVrxrVc   (12)

Δμc'/RT=lnνc'xcVc+νr'VcxcVrxr(y−1)+νc'VcVrxc−1+xcVc1V'−1Vr+Vcxca

+z21+2δε12ε1T+2ln1+g121+g12expδε12εT11−bνr'2νcVrxrVc     (13)

Isotropic phase

Δμr/RT=lnvrxrVr+vr(xr−1)+vcxr1−VrVcxc+xrVV−1+xr(Vr−1)ln1−1V

+z21+2δε12ε1T+2ln1+g121+g12expδε12εT1−b1−bνr2νr2xc

(12)

Δμc/RT=lnνcxcVc+νrVcxcVr1−1xr+νcVVrxc−1+xcVc1V−1Vr

+xcVc−1ln1−1V

1−b1−bνr2νr2xc   (13)

# Results and Conclusions

We propose a new molecular-thermodynamic frame work to describe phase behaviours of nematic liquid crystal and polystyrene systems taking into account the specific interactions. The specific interaction concept between molecules is employed from the work reported by ten Brinke and Karasz. The model gives slightly better agreement with experimental data than that of Dorgan’s. It is likely that the deficiency is basically responsible for the discrepancy between the proposed model and experimental data.

# References

1. P. J. Flory and G. Ronca, Mol. Cryst. Liq. Cryst. , 54 , 311(1979)

2. P. J. Flory and G. Ronca, Mol. Cryst. Liq. Cryst. , 54 , 289(1979)

3. M. Ballauff , Mol. Cryst. Liq. Cryst. , 136 , 175(1986)

4. J. R. Dorgan and D. S. Soane , Mol. Cryst. Liq. Cryst. , 188 , 129(1990)

5. P. J. Flory , Macromolecules , 11 , 1138(1978)

6. M. Ballauff and P. J. Flory , Ber. Bunsegas Phys. Chem. , 88 , 550(1984)

7. P. J. Flory and P. Irvine, J. Chem. Soc. Faraday Trans.I. , 80 , 1807(1984)

8. I. C. Sanchez, R. H. Lacombe, Macromolecules 11, 1145(1978)

9. I. C. Sanchez, A. C. Balazs, Macromolecules 22, 2325(1989)