- 비이온성 고분자 흡착제를 이용한 아미노산 및 항생제의 흡착

- 양우철, 심왕근, 이재욱*, 문 희

- 전남대학교 응용화학부

*서남대학교 화학공학과

- Adsorption of Amino acids and Antibiotics on Nonionic Polymeric Sorbents

- Woo Chul Yang, Wang Geun Shim, *Jae Wook Lee, Hee Moon

Faculty of Applied Chemistry, Chonnam National University, Kwangju 500-757

*Department of Chemical Engineering, Seonam University, Namwon 590-170

- Introduction

Amino acids and biochemicals have an important role in many fields. The production of these biochemicals are mainly produced by microbial fermentation processes. They are separated from the fermentation broth by complicated and costly ion exchange schemes due to low concentration and very low solubility in organic media. Such biochemicals are usually amphoteric. They exist both as anions and cations, depending upon the solution pH. Therefore adsorption and desorption of these biochemicals from ion-exchange resins may be carried out by adjusting the solution pH.

Ion-exchange has been the most widely used technology in various stages of the separation process for the industrial production[1]. Although adsorption capacities of nonionic polymeric sorbents are less than that of an ion exchanger, the desorption step may be easier and faster than the case when one employs an ion exchanger. Therefore, it is meaningful to investigate the adsorption equilibria, kinetics and dynamics of amino acids in detail[2].

In this work, the equilibrium amounts for amino acids such as phenylalanine, tryptophan and cephalosporin C on nonionic polymeric sorbents are measured in terms of pH, temperature, organic solvents and hydropobicity of sorbents.

- Experimental

The nonionic polymeric sorbents used in this study were XAD-4 and XAD-16 a macroreticular and spherical polystyrene resin cross-linked with DVB(divinylbenzene) which was supplied by Rohm and Haas Co. (Spring House, PA). Their physical properties are listed in Table 1.

The amino acids encountered in this study were L-phenylalanine(Phe),L-tryptophan(Trp) and for a comparison the antibiotics cephalosporin C(CPC) were used. These amino acids were obtained in crystalline forms from Junsei Chemical Co.(Japan) and Kanto Chemical Co.(Japan) and CPC supplied by Cheil Food & Chemicals Inc(Korea) and used without further purification. The properties of amino acids and CPC are listed in Table 2.

Adsorption amounts were obtained by a batch method. Preweighed amounts of hydrated adsorbent(~1g dry basis) were placed in test tubes containing 15ml of a solution with a known initial solute concentration. The tubes were then placed in a laboratory rotator and rotated end-to-end for a minimum of 24h in a temperature-controlled oven. From preliminary experiments, this period of time was found to be sufficient to reach equilibrium. A sample of liquid was withdrawn from the tube and, after determining the residual solute concentration in the liquid, the amount of solute adsorbed was obtained from a material balance. Experiments were carried out at different solution pH values.

A UV spectrophotometry(Varian, model DMS 100s) with 1mm path length quartz cuvettes was used to determine the concentration of Phe, Trp, and CPC at 254, 275 and 260 nm, respectively. Also, solution pH was measured by pH meter(Orion, 920A).

Table 1. Properties of Nonionic Polymeric Sorbents

| Adsorbent | # Unit | XAD-4 | XAD-16 |
| --- | --- | --- | --- |
| Chemical structure* | - | Divinylbenzene | Divinylbenzene |
| Particle size* | ㎛ | 490-690 | 560-710 |
| Particle porosity* | - | 0.51 | 0.55 |
| Moisture content | % | 58.27 | 68.96 |
| Surface area ( BET ) | m2/g | 834.6( ≥750*) | 921.6( ≥800*) |
| Average pore diameter | nm | 4.76 | 8.54 |
| Specific gravity* | - | 1.01-1.03 | 1.015-1.025 |

* from the manufacturer’s report

Table 2. Properties of Amino acids and Cephalosporin C used at 25 oC.

| Property | Phe | Trp | CPC |
| --- | --- | --- | --- |
| Molecular form | C9H11NO2 | C11H12N2O2 | C16H21N3O9S |
| Solubility in Water (kg/m3) | 29.6 | 12 |  |
| Molecular weight | 165.19 | 204.23 | 415.44 |
| pK1 | 1.83 | 2.83 | 2.6 |
| pK2 | 9.13 | 9.39 | 3.1 |
| pK3 | - | - | 9.8 |
| pI | 5.48 | 5.89 |  |

- RESULT& DISCUSSIONS

As illustrated in Figs. 1 and 2, adsorption amount of Trp on both XAD-4 and XAD-16 is greater than that of Phe and CPC. This fact implies that when comparing different sorbates, the more hydrophobic species are retained more strongly. The experiment data are well correlated by Langmuir equation.

q=qmbC1+bC					(1)

The Langmuir parameters, qmand b, were fitted to the data by a nonlinear least-squares fitting routine(MINPACK in the IMSL package) and listed in Table 3.

Table 3. Adsorption isotherms parameters of amino acids and antibiotic on nonionic

polymeric sorbents at 25 oC.

| Isotherm Type |  | Phe | CPC | Trp |
| --- | --- | --- | --- | --- |
| #### XAD-4 | qm | 1.857 | 0.9927 | 0.8626 |
|  | b | 0.01832 | 0.01925 | 0.234 |
|  | E(%) | 13.99 | 8.50 | 8.31 |
| #### XAD-16 | qm | 6.34 | 0.4285 | 0.9514 |
|  | b | 0.004021 | 0.05946 | 0.164 |
|  | E(%) | 6.60 | 8.19 | 3.71 |

Error(%)=100Nk=1Nqexp,k−qcal,kqexp,k

- The effects of pH on the uptake of Phe and CPC by XAD-16 are shown in Figs. 3 and 4. The effect of pH for Phe is clearly quite small over the range of pH 3-9. Because of the small effect of pH, no attempt was made to fit data as a function of pH with different isotherm parameters. However uptake of CPC on XAD-16 is greatly dependent on the solution pH. This result can be explained that the suppressing dissociation of the adsorbate acid group at the low pH enhances hydrophobic interaction with the nonionic sorbents. Also, we measured the adsorption uptake of Phe, Trp, and CPC on XAD-4 and XAD-16, respectively, as a function of temperature. From all experimental results in terms of temperature, we may conclude that physical adsorption is dominant for adsorption systems selected in this study.

## References

- Blackburn. S.,’Amino Acids and Amines”, Handbook of Chromatography, CRC Press, Boca Ration,(1983)

- Lee, J.W, Jung, H.J., and Moon, H., Adsorption of amino acids on nonionic polymeric sorbent,Theories and Application of Chem. Eng., 4(1),617(1998)

Fig. 2. Adsorption Isotherms for XAD-16

showing effects of the adsorbate at 25 oC

FFig. 1. Adsorption Isotherms for XAD-4

showing effects of the adsorbate at 25 oC

FFig. 4. Adsorption isotherms for XAD-16         showing effects of pH on the adsorption of CPC at 25 oC

FFig. 3. Adsorption isotherms for XAD-16         showing effects of pH on the adsorption of Phe at 25 oC