- 개질화된 활성탄을 이용한 수분과 유기용매 혼합물의 경쟁흡착

- 이종원1, 정흥조1, 이세일1, 이재욱1, 서숭혁2, 이후근3

- 1서남대학교 환경화학공학부

- 2계명대학교 화학공학과

- 3KAEL환경연구소

##### Competitive Adsorption of Water and Organic Vapor Mixtures

##### on a Modified Activated Carbon

- Jong Won Lee, Sae Il Lee, Heung Joe Jung, Jae Wook Lee, Soong Hyuck Suh, Hoo Kun Lee

- Faculty of Environmental & Chemical Engineering, Seonam University

Dept. of Chemical Engineering, Keimyung University

KAEL Environmental R&D Center

- INTRODUCTION

A large number of chemical compounds as toxic agents have been developed since the World War I introduction of toxic chemicals in the battlefiled. These substances can be classified according to their chemical properties into the following categories; (1) gases retained primarily by physical adsorption; (2) acidic or acid-forming gases; (3) basic or base-forming gases; (4) readily oxidizable gases; (5) readily reducible gases. Also, the U.S. Army and Air Force (Departments of the Army and the Air Force, 1975) classify chemical agents in terms of their functions and effects as follows: choking agents, never agents, blood agents, blister agents, vomiting agents, and tear agents. Activated carbon is not effective for the removal of toxic chemical agents such as phosgene, hydrogen cyanide, arsine, etc. from ambient air. However, adsorption capacity to retain these agents can be significantly improved by impregnating it with certain metal compounds. With the presence of proper impregnants, retention of toxic gases by carbon is enhanced because of the reactions between toxic gas and the impregnants. For the purpose of removing toxic chemicals, one is concerned primarily with the adsorption capacity of adsorbents and the certainty that adsorbed toxic agents will be strongly held and not desorbed. These objectives may be achieved by impregnating activated carbon with certain metal compounds.

Activated carbons are very often used as adsorbents from gaseous mixtures containing water vapors such as air. It is well-known that moisture in air may play a role in a competitive adsorption of a pollutant. The mechanism of water adsorption was proposed by Dubinin and Serpinsky. Their interpretaion of the shape of experimental isotherms is based on interactions of water molecules with either pure carbon- or oxygen-containing surface species. According to DS theory water molecules are first adsorbed on primary adsorption centers, adsorbed water molecules, occurs. Thus an increase in the water vapor pressure leads to the formations of clusters of associated posed that below p/p0=0.3. Surface chemistry governs the adsorption process, while at higher relative pressure microporosity becomes an important factor. The number of primary adsorption centers can be calculated by fitting the experimental isotherm to the equation formulated by Dubinin and Serpinsky (DS).

Many experimental results along with their interpretation have been published based on DS approach. In some cases, especially for carbons with a large number of chemical groups, the attempts to fit the experimental data to the proposed isotherm failed. Recently some research groups have been proposed modified DS isotherm to correlate the adsorption equilibrium data of water vapor on activated carbon.

In this work, an experimental study for the adsorption of water vapor and organic gas mixtures was investigated in a fixed-bed column charged with manufactured impregnated activated carbon. Among organic gases, carbon tetracloride (CCl4) and acetone were chosen as a reference of nonpolar and polar gases. The physical and chemical properties of impregnated activated carbon were characterized by the instrumental analysis such as BET, TG/DTA and SEM-EDS. Adsorption capacity of water vapor was measured at 308.15 K and analyzed by means of the two Dubinin-Serpinski (DS) equations and a third similar equation, based on the same principles. Column dynamics of single and binary system of water and organic vapors were studied experimentally.

## Adsorption Isotherm

### It has been postulated for a long time that the characteristic sigmoid-shaped isotherm exhibited by water vapor adsorption on carbon surfaces can be rationalized by assuming that adsorption initially occurs on primary sites, comprised of chemisorbed oxygen compounds, and that further adsorption takes place on these hydrated sites by the formation of hydrogen bonds. Dubinin and Serpinski proposed two isotherm equations to correlate sigmoid-shaped isotherm of water vapor.

q=q0cpp01−cpp0							(1)

### cq0+q1−kq=qpp0					(2)

### Comparing with the DS equation (Barton et al., 1992), the following simple isotherm model has the advantages of expressing q explicitly as a function of P/P0 and containing three instead of four isotherm parameters.

q=q01+expkp50p0−pp0					(3)

where p50 = an isotherm parameter; and p=p50 at q/q0=0.5. The plot of Eq. (3) exhibits a characteristic S shape with P50 at q/q0=0.5 as an inflection point.

## EXPERIMENTAL

The activated carbon of 14~30 mesh (Supplied by Samchuli Co., Korea) was used as a base adsorbent. Activated carbon was prepared through the impregnation in a batch reactor. The adsorbent was immersed into the aqueous ASC solution for one hour at room temperature. The ASC solution was composed of CuCO3, Cu(OH)2, CrO3, AgNO3, NH4OH, and (NH4)2CO3. After these treatments, the activated carbon was dried at 90oC for the activation for 1 hour and at 150oC for 2-3 hours. Organic gases of CCl4 and acetone are produced from an evaporation of aqueous solution. The gas-phase concentration is adjusted by controlling the solution temperature and the nitrogen flow rate. Nitrogen was used as a carrier gas at 100-250 ml/min. All parts of the system, such as the adsorption column, mixing baffle and gas flow lines, were made of glass and pyrex. The temperature inside the adsorbent was controlled by water bath. A constant amount of the adsorbents is packed in a column with a dimension of 0.01 m I.D. by 0.4~0.2 m length, and these adsorbents were thermally equilibrated with the gas-phase. The effluent concentration of toxic gases from the column was analyzed by the gas chromatography with a thermal conductivity detector (TCD) and Porapack-Q column at an oven temperature of 140oC.

.

## RESULT & DISCUSSIONS

In order to investigate the physical and chemical properties of both base activated carbon and modified activated carbon using metals such as Cu, Ag and Cr, some instrumental analyses were conducted. The surface area and pore size distribution were measured by BET-N2 analysis (Micromeritics, ASAP 2400) for both adsorbents. The determined surface area was to be about 1300 m2/g and the average pore size is 18Å. In addition, TG/DTA and SEM-EDS analysis were conducted to investigate the thermal stability and impregnation state. Fig. 1. shows the sigmoid-shaped adsorption isotherm of water vapor on impregnated activated carbon. Adsorption capacity was measured at 308.15 K and correlated by modified Dubinin-Serpinski (DS) equation. As listed in Table 1, the isotherm parameters were extracted using multivariable, nonlinear regression. In this regard, a modified Lezenverg-Marquardt algorithm was used (IMSL routine DUNLSF).

Table 1. Modified DS Parameters for Water Vapor Adsorption on Impregnated AC at 308K.

| Model | Modified DS |  |  |
| --- | --- | --- | --- |
| Parameters | q0 | k | P50P0 |
| Value | 0.3034 | 8.136 | 0.5856 |

Column dynamics of single and binary system of water and organic vapors were studied experimentally. Fig. 2 shows the breakthrough curves of water vapor in terms of relative humidity(20, 40, 60%). The influences of water vapor on the adsorption of carbon tetracloride and acetone were quite different as shown in Figs. 3 and 4. In order to simulate these adsorption phenomena, further work will focus on the model development for the competitive adsorption between water vapor and organic chemicals

## References

Barton. S.S, Evans M.J.B, and MacDonald. J.A.F, “The Adsorption of Water Vapor by Porous Carbon”, Carbon, 29(8), 1099-1105 (1991)

Ruthven, D.M., Principles of Adsorption and Adsorption Process. Wiley, New York(1984)

Yang. R. T., Gas Separation by Adsorption Processes, Butterworths Boston(1987)

Fig. 1. 	Adsorption isotherm of water	  Fig. 2.	Breakthrough curves of water vapor

vapor at 308.15K.			in terms of relative humidity.

Fig. 3. 	Binary breakthrough curves of 	  Fig. 4. Binary breakthrough curves of

water and acetone vapor mixtures		water and CCl4 mixtures