광촉매를 이용한 비소화합물의 산화;비소 오염 지하수에의 응용

이현주, 최원용

포항공과대학교 환경공학부

Photocatalytic Oxidation of Arsenite in TiO2 Suspension:

# Implication for Groundwater Remediation

Hyunjoo Lee and Wonyong Choi

School of Environmental Science and Engineering, Pohang University of Science and Technology, Pohang, Kyongbuk 790-784, Korea

Arsenite [As(III)] and arsenate [As(V)] are highly toxic aquatic contaminants that pose a potential threat to the environment and human health. They are characterized by different chemical behavior, bioavailability, and toxicity. It is known that the arsenite is ca. 60 times more toxic and more mobile than arsenate. Therefore, the oxidation of arsenite to arsenate is desirable in order to reduce the arsenic toxicity while facilitating its removal from water supply.  We performed the photocatalytic oxidation of arsenite in TiO2 suspension in this study. The effects of pH, humic acids(HA), and ferric ions on the arsenite oxidation kinetics were investigated in detail. Arsenite oxidation was enhanced in the alkaline condition than in the acidic one. The addition of HA and ferric ions at pH 3 greatly increased the photocatalytic oxidation rate of arsenite.

Photocatalytic reaction proceeds through the direct h+-e- reaction or radical mediated pathway. Adsorption behaviors of arsenite and arsenate at pH 3 and 9 reveal that the direct oxidation of arsenite by h+ is insignificant. The addition of t-butyl alcohol that is an •OH radical scavenger did not reduce the rate of arsenite oxidation. Based on this observation, we propose that the superoxide(O2•-) plays the role of the main oxidant of arsenite in this photocatalytic system as follows.

As(III) + O2•-  → As(IV) + H2O2

As(IV) + O2  →  As(V) + O2•-

Added HA acts as an effective electron donor to generate superoxide, which mediates the oxidation of arsenite. On the other hand, addition of ferric ions enhanced the photocatalytic oxidation of arsenite by producing •OH radicals from the photolysis of Fe(OH)2+ species. The optimal concentration of ferric ions was around 0.5 mM. Since Fe3+ and HA effectively enhanced the photocatalytic oxidation of arsenite, the arsenic contaminated groundwater that often contains high concentration of iron or organic matter could be readily remediated by the photocatalytic method.