연소/소각 배가스 분위기에서 표면개질활성탄상에

NOx-SO2 의 선택적 흡착 거동

이영환, 최병욱, 윤정호*, 정재훈, 장성철, 최대기, 박진원**

한국과학기술연구원 환경공정연구부, AspenTech Ltd.,연세대학교 화학공학과*

- Selective Adsorption Behavior of NOx-SO2 on Surface Modified Activated Carbon

- in Combustion/Incineration Flue Gas Condition.

Young-Whan Lee, Byoung-Uk Choi, Jeong-Ho Yun*, Jae-Hoon Choung, Seong-Cheol Jang, Dae-Ki Choi, Jin-Won Park**

Environment and Process Technology Div., KIST

Aspen Engineering Suite, AspenTech Ltd. in U.K*

Dept. of Chemical Engineering, Yonsei University**

- Introduction

- Human health effects and material damage from corrosive acidic species like SO2 and NOx are confined to local regions around pollution sources.  In general, combustion flue gas lives in a low temperature atmosphere of 373-423 K with about 1000 ppm of NOx and SO2 respectively and an excessive amount of O2 is definitely included. NOx has a 7:1-10:1 ratio of NO to NO2. The advantages of processing combustion flue gas using general activated carbon are based on the fact that not only NOx and SO2 are removed, but noxious substances such as hydrogen fluoride (HF), hydrogen chloride (HCl), mercury (Hg) included in the combustion flue gas are removed at the same time.  Also, because industrial water is not used, secondary pollution is not the outcome and useful by-products can be obtained during this process.  Noxious substance removal using general activated carbon based on the physisorption, to this day, is still reported to have very low selective removal efficiency with the exception of volatile organic compounds. This is the reason for not using this method despite many advantages such as having high surface area, unique pore structure, economical factor, etc

We have proposed a mechanism in our previous study (Lee et al., 2001) using K-IAC to NOx and SO2 by conducting a research on surface chemistry along with the adsorption characteristics.  ToF-SIMS and AES/SAM were used as surface analysis methods for the first time in our previous study to define surface chemistry with NOx and SO2 adsorbed impregnated activated carbon and we were able to collect a great deal of information.  Related studies until recently have reported that when pure-component adsorption is conducted for both NOx and SO2 using KOH impregnated activated carbon (K-IAC), both showed several times to several tens of times higher selectivity compared to general activated carbon.  However, there were almost no reports doing research on simultaneous adsorption of the binary-component with NOx-SO2 using K-IAC, especially no study on surface chemistry exists.  During the recent years, studies on the surface group of the activated carbon itself were conducted with great interest, but the characteristics of the activated carbon surface group and its accurate amount is known to be very difficult to analyze.  The surface, in particular, has many pores in irregular sizes and roughness making the analysis all the more difficult.  To understand and use impregnated activated carbon appropriately, it is most important that the chemical characteristics as well as the selective adsorption behavior of the surface are accurately identified.

- This study, therefore, aims at identifying the simultaneous adsorption characteristics of NO, NO2 and SO2 in the combustion flue gas condition using KOH impregnated activated carbon and defining the surface chemistry under the condition.

Experimental

The adsorbent was prepared by impregnating a KOH (Junsei Chemical Co.) solution into granular activated carbon (GAC) obtained from coconut shell (Dongyang Carbon Co.).  GAC was sieved through a 8/16 mesh and treated with N2 flowing for 4 h at 413 K.  Next the treated GAC was dried at 383 K.  KOH was impregnated in an aqueous solution state in the GAC via incipient wet impregnation, and was used following dehydration at 403 K.  Manufactured K-IAC was stored in a desiccator from common airborne moisture and contaminants to prevent adsorbent function reduction.  At this time, cautions were taken for impregnation, drying, and storage of adsorbent because the processes have a great influence on the adsorption capacity.  Through atomic absorption spectroscopy (AAS) analysis, potassium loading of K-IAC was confirmed to be 9.96 wt. %.

The fixed-bed adsorption system used in this experiment is shown in Figure 1. The fixed-bed adsorption column was a 316 stainless steel tube, with an inside diameter of 10.9

Figure 1.  Schematic diagram of fix-bed adsorption system for noxious gas control

mm and a length of 400 mm.  Inside the columns, steel mesh was placed in the upper and lower extremities of the adsorbent to support the samples and minimize channeling phenomenon.  The temperature of the column was maintained with an electric furnace located at its outer wall.  For the system line, the temperature was maintained by using a heat band and heat insulating material and was regulated with a proportional-integral-differential (PID) temperature controller.  The temperature was measured by connecting a K-type thermocouple (Omega Engineering Inc.) located inside the line and connected to a recorder.  Each certified 2% NO/N2 , 5000 ppm NO2/N2, 2% SO2/N2, high purity O2 was diluted to the desired concentration range via a mass flow controller (Brooks Co., model 5280E).  In the fore-end of the adsorption column, an in-line static mixer was installed to facilitate mixing.  Concentrations of NO, NO2 and SO2 that exhausted from the bypass line and adsorption column were analyzed by using a chemiluminescent NOx analyzer (Thermo Environmental Instruments Inc., model 42C) and a flue gas analyzer (Eurotron Instruments S.p.A., GreenLine Mk II) for SO2, CO and O2 analysis.  Daily NOx, and SO2 analyzer calibrations were performed with N2 (zero value) and NO, NO2, and SO2 gases certified by manufacturer analysis having a concentration of near 80% of the analyzer full-scale range (span value).  During the adsorption experiment, analysis on column outlet concentrations of NO, NO2, NOx (NO+NO2), SO2, CO and O2 is controlled with software.  Analytical data are captured every minute and read into a computer, generating 300 analytical values from every of 300-minute-long experiment.  Detailed conditions of each experiment are shown in Table 2.

The surface chemical analysis was performed for samples by utilizing XRD (Rigaku, D/MAX-III A), AES/SAM (Perkin-Elmer, PHI Model 670), and static type ToF-SIMS (Perkin-Elmer, PHI Model 700 ToF-SIMS/SALI), XPS (PHI).

Results and Discussion

All experiments (Figure 2-4) shows the concentration curve of NOx and SO2 emitted from the column outlet after adsorption of 891 ppm NO, 116 ppm NO2, 1004 ppm SO2 and 18.1% O2 to K-IAC for 5 h.  The adsorbent amount was 10.6730g, reaction temperature was 403K, flow rate was 1.68 L/min, and linear velocity of 30 cm/sec with the contact time at 0.67 sec.  In the adsorption behavior and surface chemical results, it was noticed that oxide crystal was produced partially because of NOx as SO2 with stronger adsorption affinity became dominant in most of the selective adsorption site when SO2 and NOx (NO:NOx=7.7:1) coexisted in K-IAC.  It was also noted that a large amount of oxygen was chemisorbed.   From depth information of surface (Figure 5), SOx- also decreased in larger amounts than NOx-.  Meanwhile, amounts of OH- and KO- in KOH as selective adsorption site were reduced.  The NOx and SO2 adsorption on K-IAC took place by the chemical reaction between impregnant (KOH) and adsorbates (NOx and SO2), which clearly explains the fact that KOH was gradually losing its function as the selective adsorption site by NOx and SO2 adsorption.  When NOx-SO2 coexist, competitive adsorption occurs, losing more OH- and KO-, as secondary ions of selective adsorption site due to ToF-SIMS resulting from the reaction between KOH and SO2.  Cx- and CHx- are groups mainly formed on the existing activated carbon surface and these groups provide positive evidence that K-S-O and K-N-O are concentrated near the external surface.

- Referenece

[1] Guo, J. A.; Lua, C. Microporous and Mesoporous Materials 32, 111 (1999).

[2] Lisovskii, A.; Semiat, R.; Aharoni, C. Carbon, 35, 1639 (1997).

[3] Lizzio, A. A.; DeBarr, J. A.: Energy Fuels, 11, 284 (1997).

[4] Forzatti, P., Nova, I., Beretta, A.: Catal. Today, 56, 431 (2000).

[5] Lapina, O. B., Bal’zhinimaev, B. S., Boghosian, S., Eriksen, K. M., Fehrmann, R.: Catal. Today 51, 469 (1999).

[6] Illán-Goméz,M. J., Brnadán, S., Linares-Solano, A., Salinas-Martínez de Lecea, C. Appl. Catal. B, 25, 11 (2000).

[7] Zhu, Z. H. Lu, G. O. : J. Catal. 187, 262 (1999).

[8] Lott, S. E;. Gardner, T. J.; McLaughlin, L.I.; Oelfke, J. B.; Matlock, C. A. : US Patent 5,795,553, August 18, (1998).

[9] Boehm, H. P.: Discuss. Faraday Soc. 52, 264 (1972).

[10] Vickers, P. E., Castle, J. E., Watts, J. F. Appl. Sur. Sci. 150, 244 (1999).

[11] Lamontagne, B.; Semond, F., Adnot, A., Roy, D.:  Appl. Sur. Sci., 90, 447 (1995).

##### [12] Roy, C., Darmstadt, H., Benallal, B., Amen-Chen, C.: Fuel Processing  Technology, 50, 87 (1997).

[13] Vladea, R. V.; Hinrichs, N.; Hudgins, R. R., Suppiah, S., Silveston, P. L. Energy Fuels  11, 277 (1997).

[14] Lee, Y. W., Choi, D. K., Park, J. W. : Ind. Eng. Chem. Res. 40, 3337 (2001).

[15] Lee, Y. W., Choi, D. K., Park, J. W. : in press, Sep. Sci. Technol. (2001).

[16] Lee, Y. W., Choi, D. K., Park, J. W.: in revision, Carbon (2001).

[17] Lee, Y. W., Choung, J. H., Choi, D. K., Park, J. W.: in revision, Env. Sci. Technol. (2001).

[18] Lee, Y. W., Choung, J. H., Choi, D. K., Park, J. W.: submitted to Adsorption. (2001).

[19] Lee, Y. W., Jang, S. C., Choung, J. H., Lee, J. H., Choi, D. K., Park, J. W., Yun, J. H: submitted to AICHE (2001).

[20] Lee, Y. W., Choung, J. H., Choi, D. K., Park, J. W.: 7th international conf. on fundamental of adsorption (FOA7). Nagasaki: International Adsorption Society, 185 (2001).

[21] Lee, Y. W., Choung, J. H., Choi, D. K., Park, J. W.: 4th international symp. Effects of surface heterogeneity in adsorption and catalysis on solids (ISSHAC IV),Cracow, Poland,  (2001).

##### Figure 3. O2 Concentration profile for binary-component adsorption of NOx-SO2.

##### Figure 2. CO Concentration profile

##### for binary-component adsorption of NOx-SO2 .

##### Figure 4. NOx and SO2 Concentration profile  for adsorption of NOx-SO2 binary system.  Gas composition :  891 ppm NO, 116 ppm NO2, 1004 ppm SO2,  18.1 % O2.  T=403 K.  L.V. =29.971 cm/sec.

##### Figure 5. Depth distribution of (a) SOx- and (b) NOx- ions obtained K-IAC adsorbed for 5h with 1007 ppm NOx and 1004 ppm SO2 at 403K.